# Part No.﹕1L0545W21A0CB201

§  Standard 5mm diameter package.

Characters

§  High intensity.

## Outline Dimensions

§  All dimensions are in millimeters（inches）.

§  Tolerance is ±0.25（.010）㎜ unless otherwise noted.

§  Protruded resin under flange is 1.0㎜（.04）max.

Absolute Maximum Ratings（Ta=25℃）

| ###### Item | ###### Symbol | Value | ###### Unit |
| --- | --- | --- | --- |
| Power Dissipation | PD | 120 | mW |
| DC Forward Current | IF | 30 | mA |
| Pulsed Forward Current | IFP | 100* | mA |
| Reverse Voltage | VR | 5 | V |
| Operating Temperature | Topr | -25 ~ +80 | ℃ |
| Storage Temperature | Tstg | -40 ~ +100 | ℃ |
| Soldering Temperature | Tsol | 260for5sec | ℃ |

* Duty 1/10  Pulse Width 0.1ms   △ At the position of 4mm from the bottom

of the package

Electrical-Optical Characteristics（Ta=25℃）

| ITEM |  | MATERIALS |
| --- | --- | --- |
| Resin(Mold) |  | Epoxy |
| Lens Color Code | C | Water Transparent |
|  | T | Colored Transparent |
|  | M | White Diffused |
|  | D | Colored Diffused |
| Lead Frame |  | Ag Plating Iron Alloy |
| Dice |  | InGaN |

Directive Characteristics（Ta=25℃）

| Parameter | ###### Symbol | ##### Value |  |  | ##### Unit | ##### Test condition |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | Min. | Typ. | Max. |  |  |
| Forward Voltage | Vf | ﹍ | 3.2 | 4.0 | V | If=20mA |
| Luminous intensity | Iv | 420 | 550 | ﹍ | mcd | If=20mA |
| Wavelength | X(&λd) | ﹍ | 0.2938 |  | (nm) | If=20mA |
|  | y | ﹍ | 0.2879 | ﹍ | ﹍ | If=20mA |
| Reverse Current | Ir | ﹍ | ﹍ | 1 | μA | Vr=5V |
| Viewing angle | 2θ1/2 | ﹍ | 120 | ﹍ | Deg | If=20mA |
| Spectral half bandwidth | △λ | ﹍ |  | ﹍ | nm | If=20mA |